Media release

## Small-scale MX Kneader for development of compounds

BUSS: Laboratory kneader with four-flight technology

Pratteln (Switzerland), April 2012 –  Making its trade fair début on the exhibition stand of Buss AG, Pratteln (Switzerland), at NPE 2012 in Orlando/USA (2th to 5th April 2012) will be this company’s four-flight Laboratory BUSS Kneader MX 30. The MX 30 completes the range of four flight MX compounding units. Featuring a flanged-on discharge screw, the laboratory BUSS kneader is rated for output rates of 5 to 25 kg/hour respectively for batch quantities upwards of 300 g. It has a maximum screw speed of 800 r.p.m.

Visitors to the BUSS stand (Nr. 7463 in West Hall) will be able to view the kneader with its barrel housing in the opened position permitting a clear observation of the working of the four-flight co-kneader, namely the dual rotational and oscillating motion of the screw and its combined axial and transverse mixing action, which together ensure an extremely high quality of mix.

Designed specially for research and development applications as well as process and formulation development and optimization, the MX 30 is the first laboratory kneader to feature four-flight technology. Like the larger machines of the MX series, the MX 30 is particularly suitable for the compounding of heat-sensitive and shear-sensitive polymers and for the production of highly filled compounds. Typical areas of application in the highly diversified cable compound industry are:

Halogen-free, flame-retardant (HFFR) cable compounds; during the compounding process, the temperature of the melt must be kept below 180 °C – at any higher temperature the flame retardant ATH (alumininum trihydrate; Al(OH)3), which is incorporated into the base material in quantities of between 55 and 70% w/w, will begin to decompose.

Peroxide-crosslinking polyethylene (XLPE) for cable insulation; here the maximum permissible temperature during the compounding process is even lower – only 125 °C, as any higher temperature could trigger peroxide decomposition and crosslinking reactions.

Silane-crosslinkable cable compounds – the liquid silane is injected straight into the polmer melt by way of a special injector, primarily in applications where the compound is to be used for the insulation of low-tension cables and, in addition, has to be provided with flame-retardant properties, this now being a more frequent requirement.

Semiconductive polyolefin compounds for power cables containing up to 40% w/w conductive carbon black. These materials typically have very low apparent density and must be metered into the kneader with absolute precision and homogeneously mixed into the melt with optimum shear and without destroying its structural properties.

A comprehensive range of accessories, e.g. metering systems for raw materials and different pelletizers, make this laboratory BUSS kneader a versatile and fully equipped small-scale compounding line that can be used not only for product development trials but also for the production of sample quantities for customers’ own trials or for the small-batch production of a wide diversity of cable compounds.



Contact person for further information:

Marco Senoner, Buss AG
	Hohenrainstrasse 10, CH-4133 Pratteln
	Tel.:  +41(0) 61/825 65 51,  Fax:  +41(0) 61/825 66 88
	E-mail:  marco.senoner@busscorp.com
	Internet:  http://www.busscorp.com

Contact person for editorial material:

Dr. Diether Burkhardt,  KONSENS Public Relations GmbH & Co. KG,
	Hans-Kudlich-Straße 25,  D-64823 Groß-Umstadt
	Tel.:  +49(0) 60 78/93 63-0,  Fax:  +49(0) 60 78/93 63-20
	E-mail:  mail@konsens.de

Dear colleagues, 
You can download this press release in German, English, and Spanish with 
the colour photo in high-resolution print quality at:
http://www.konsens.de/buss/.html

The first Buss laboratory machine to feature four-flight technology:  Designed for product batches upwards of 300 g, the Laboratory BUSS Kneader MX 30, shown here with three material feed systems and a discharge screw, is suitable for the development of formulations and processes, especially for the production of cable compounds 
Photo: Buss AG, Pratteln, Switzerland