New plastomer for direct processing or PP modification:
Koattro KT AR05 is soft and flexible

Augsburg, March 2010

A recent addition to Ultrapolymers’ (www.ultrapolymers.de) portfolio of high performance polymers is LyondellBasell’s Koattro KT AR05 plastomer for direct processing or use as a modifying agent for polypropylene. Uncured and without the need for any plasticiser, this material combines high flexibility (bending stiffness 20 MPa) with an outstanding low compression set at high temperatures of 42 % at 70 °C, and a very high level of ductility (elongation at break >400 %). A melt flow rate of 0.5 g/10 min (190 °C, 2.16 kg) and its high melt stability allow this new plastomer to be converted to films, profiles, containers or parts using all common manufacturing processes for thermoplastic polymers. Its low Shore A hardness of 77 results in soft-touch surfaces. PP modified with Koattro KT AR05 shows significantly reduced stress whitening.

In certain applications the new plastomer can substitute styrene-block-copolymers, which have a higher density and, due to their cured molecular structure, are more difficult to recycle. Being non-toxic and approved for food contact, seals and gaskets for closing systems are a large potential area of application. Beyond this,  Koattro KT AR05 is well suited to foaming processes, facilitating the manufacture of flexible sheets with a density of 650 g/cm³ and a compression set of only 9.2 % at 23 °C.

When used as modifier for PP, Koattro KT AR05 significantly reduces the material’s stress whitening, compression set, hardness and rigidity, whilst at the same time increasing its elongation at break, toughness, and transparency. This helps, for example, to preserve the shelf appeal of a highly transparent injection moulded or thermoformed container even after rough handling during transport and storage. Similar benefits are gained with flexible automotive parts, which require extensive bending for assembly.

The newly-developed grade KT AR05 is the first commercially available member in a growing family of Koattro plastomers by LyondellBasell. Among other grades to follow is a high flow grade for injection moulding, which is already available for trial purposes. A highly transparent metocene grade is also currently under development.

Koattro is a trademark of LyondellBasell

Ultrapolymers Deutschland GmbH, Augsburg/Germany, supplying customers in Germany, Austria and Switzerland, is part of the pan-European plastics distributor Ultrapolymers Group NV, Lommel/Belgium. The company’s portfolio includes polyolefines from LyondellBasell, polystyrene from INEOSNOVA, polyamide from Ascend and Ravago, long fibre reinforced thermoplastics, bio-based polymers from FKuR, rotational moulding polymers from LyondellBasell, engineering polymers from LG Chem, commodities, masterbatch and additives, the Colorflexx service package for self-colouring of ABS as well as customer specific compounds. Headquartered in Augsburg, Ultrapolymers Deutschland runs sales offices in Bielefeld, Kierspe, Nurnberg, and Stuttgart. Austrian and Swiss customers are supported from the distributor’s Augsburg office.

| Voucher copies and editorial contact: Konsens PR GmbH & Co. KG, Dr. Jörg Wolters, Hans-Kudlich-Str. 25 D-64823 Groß-Umstadt Tel.: +49 (0) 60 78/93 63-13 E-Mail: mail@konsens.de | Please find this press release as Word file for download under: http://www.konsens.de/ultrapolymers.html |
| --- | --- |

Koattro KT AR05 is a newly developed plastomer from LyondellBasell for direct processing or use as a modifier for polypropylene. Blended with a common PP-HeCo grade this recent addition to Ultrapolymers’ portfolio increases the surface gloss, transparency, puncture and tear resistance of films, whilst at the same time decreasing their stiffness and increasing their flexibility.

Graph: Ultrapolymers

Please find this image in printable resolution for download under:
http://www.konsens.de/ultrapolymers.html