NEWS RELEASE

New ZnO PRO vulcanization accelerator for greater sustainability and cost efficiency

The new range of ZnO PRO vulcanization accelerators from BrüggemannChemical combines previously unattained cost efficiency with high effectiveness and increased sustainability due to the very low content of zinc and other heavy metals in the end-product.

Heilbronn, Germany, December, 2016 – BrüggemannChemical (www.brueggemann.com), a specialist for zinc-based additives used in the vulcanization of rubber, has developed a new range of reaction accelerators with its ZnO PRO series. The products, which are produced by a wet chemical process, combine the latest findings in rubber compounding with lower costs and reduced heavy metal content. At the same time, they allow the direct substitution of conventional thermal zinc oxide without the need to modify the formulation or make compromises on performance. ZnO PRO is suitable for the entire range of application of sulfur-vulcanizable rubber – from technical parts and consumer goods to tires.

At present, the new product range comprises the A250 (the lowest-price type), the R260 and the A280. All three new products result in vulcanizates with a high crosslinking density and uniform mechanical properties. They are also readily dispersible. As regards the attainable vulcanization level, A250 more or less corresponds to the existing industry standard Red Seal that causes considerably higher costs, while the other two are significantly more effective than Red Seal despite their favorable price. This means that the members of the ZnO PRO series offer currently the best cost-to-benefit ratio in this class. The special formulations for the relevant types result in comparatively low heavy metal contents in the end product, ranging from below 1.0 % with A280 and R260 (1.6 % for Red Seal) to less than 0.6 % with the A250 type. The ZnO PRO series thus supports the striving for greater sustainability known in the elastomer sector as "Green Rubber".

Fully equipped Technical Center for in-house and customer developments 
Only recently, BrüggemannChemical opened its new Technical Center, fully equipped with the very latest machines and systems. These include a Banbury internal mixer, a mixing mill, a vulcanizing press and a variety of testing devices to determine the processing, vulcanization and performance properties of elastomers. A major role is played there by the tailor-made, application-oriented optimization and synthesis of zinc-based activators – for example of the ZnO PRO series – for in-house developments and on the customer's behalf. With the possibility of driving developments jointly with its customers and being able to comprehensively and immediately test the result, the company is underlining its outstanding industry-wide R&D competence as an additives producer in the rubber segment.

BrüggemannChemical L. Brüggemann KG is a renowned manufacturer of specialty chemicals with some 200 staff. Founded in 1868, the company, headquartered in Heilbronn, Germany, specializes in developing and manufacturing high performance additives for engineering thermoplastics with a focus on polyamides, as well as zinc derivatives and sulfur-based reducing agents. Customers from more than 60 countries have come to value the company's flexibility and innovative product solutions, while subsidiaries in the USA and Hong Kong emphasize its international outlook. The cornerstones of corporate policy are in-house research and development activities, a consistent focus on customer requirements, and major investment in know-how and plant.

■■■

# Weitere Informationen:

Gunther Spiess, Sales & Marketing Manager Zinc Derivatives

BrüggemannChemical L. Brüggemann KG, Salzstraße 131, D-74076 Heilbronn

Tel.: +49 (0) 71 31 / 15 75 – 294, Fax: - 25 294
E-Mail: gunther.spiess@brueggemann.com

# Redaktioneller Kontakt, und Belegexemplare bitte an:

Dr.-Ing. Jörg Wolters, Konsens PR GmbH & Co. KG,

Hans-Kudlich-Straße 25,  D-64823 Groß-Umstadt – www.konsens.de

Tel.: +49 (0) 60 78 / 93 63 - 0,  Fax: - 20,  E-Mail: joerg.wolters@konsens.de

Dear colleagues,

Press releases from BrüggemannChemical including text and pictures in printable resolution can be downloaded from: www.konsens.de/brueggemann.html